# Advanced Cast Stone’s Precast Architectural Concrete Standard Specifications

Section 03450 governs the specifications for the manufacturing of precast. Advanced Cast Stone complies with the following specifications.

Section 03450

PRECAST ARCHITECTURAL CONCRETE

PART 1 GENERAL

  - SECTION INCLUDES

- Architectural precast concrete wall panels.

- Architectural precast concrete lintels, sills, copings, and trim.

- Architectural precast concrete pavers.

D. Supports, anchors, and attachments.

E. Perimeter and intermediate joint seals.

F. Grouting under panels.

  - RELATED SECTIONS

A. Section 03300 - Cast-in-Place Concrete: Building structural frame.

B. Section 03380 - Post Tensioned Concrete: Building structural frame.

C. Section 03410 - Plant-Precast Structural Concrete: Building structural frame.

D. Section 03470 - Tilt-Up Precast Concrete: Building structural frame.

E. Section 03415 - Precast Concrete Hollow Core Planks: Building structural floor.

F. Section 05120 - Structural Steel: Building structural frame.

G. Section 07620 - Flashing and Sheet Metal.

H. Section 07900 - Joint Sealers.

I. Section 04720 – Architectural Cast Stone

1.3 REFERENCES

A. American Concrete Institute.

1.   ACI 211.1 - Normal, Heavy Weight, and Mass Concrete, Practice for Selecting

Proportions; 1991.

2.   ACI 318 - Building Code Requirements for Reinforced Concrete; 2002.

3.   ACI 533R - Guide for Precast Concrete Wall Panels; 1993.

B. ASTM International.

1.   ASTM A 36/A 36M - Standard Specification for Carbon Structural Steel; 2001

2.   ASTM A 47/A 47M - Standard Specification for Ferritic Malleable Iron Castings; 1999.

3.   ASTM A 123/A 123M - Standard Specification for Zinc (Hot-Dipped Galvanized)

Coatings on Iron and Steel Products; 2002.

4.   ASTM A 153/A 153M - Standard Specification for Zinc Coating (Hot Dip) on iron and

Steel Hardware; 2002.

5.   ASTM A 185 - Standard Specification for Steel Welded Wire, Fabric, Plain, for

Concrete Reinforcement; 2001.

6.   ASTM A 283/A 283M - Standard Specification for Low and Intermediate Tensile

Strength Carbon Steel Plates; 2000.

7.   ASTM A 307 - Standard Specification for Carbon Steel Bolts and Studs, 60,000 PSI

Tensile Strength; 2002.

8.   ASTM A 325 - Standard Specification for Structural Bolts, Steel, Heat Treated,

120/105 ksi Minimum Tensile Strength; 2002.

9.   ASTM A 325M - Standard Specification for High Strength Bolts for Structural Steel

Joints; 2000

10. ASTM A 416/A 416M - Standard Specification for Steel Strand, Uncoated Seven-Wire

for Prestressed Concrete; 1999.

11. ASTM A 496 - Standard Specification for Steel Wire, Deformed, for Concrete; 2001.

12. ASTM A 500 - Standard Specification for Cold-Formed Welded and Seamless Carbon

Steel Structural Tubing in Rounds and Shapes; 2001a.

13. ASTM A 563 - Standard Specification for Carbon and Alloy Nuts; 2000.

14. ASTM A 572/A 572M - Standard Specification for High-Strength Low-Alloy

Columbium-Vanadium Structural Steel; 2001.

15. ASTM A 615/A 615M - Standard Specification for Deformed and Plain Billet-Steel

Bars for Concrete Reinforcement; 2001b.

16. ASTM A 767/A 767M - Standard Specification for Zinc-Coated (Galvanized) Bars for

Concrete Reinforcement; 2000b.

17. ASTM A 934/A 934M - Standard Specification for Epoxy-Coated Prefabricated Steel

Reinforcing Bars; 2001.

18. ASTM C 33 - Standard Specification for Concrete Aggregates; 2002a.

19. ASTM C 39/C 39M - Standard Test Method for Compressive Strength of Cylindrical

Concrete Specimens; 2001.

20. ASTM C 150 - Standard Specification for Portland Cement; 2002a.

21. ASTM C 260 - Standard Specification for Air-Entraining Admixtures for Concrete;

2001.

22. ASTM C 330 - Standard Specification for Lightweight Aggregates for Structural

Concrete; 2002b.

23. ASTM C 404 - Standard Specification for Aggregates for Masonry Grout; 1997.

24. ASTM C 494/C 494M - Standard Specification for Chemical Admixtures for Concrete;

1999a.

25. ASTM C 642- Standard Test Method for Density, Absorption, and Voids in Hardened

Concrete; 1997.

26. ASTM C 979 - Standard Specification for Pigments for Integrally Colored Concrete;

1999.

27. ASTM C 1107 - Standard Specification for Packaged Dry, Hydraulic-Cement Grout

(Nonshrink); 2002.

28. ASTM C 1240 - Standard Specification for Use of Silica Fume as a Mineral Admixture

in Hydraulic-Cement Concrete, Mortar and Grout; 2003.

29. ASTM D 412 - Standard Test Methods for Vulcanized Rubber and Thermoplastic

Elastomers-Tension; 1998a.

30. ASTM F 593 - Standard Specification for Stainless Steel Bolts, Hex Cap Screws, and

Studs; 2002.

C. American Welding Society.

1. AWS D1.1/D1.3M - Structural Welding Code; 2003.

- AWS D1.4 - Structural Welding Code - Reinforcing Steel; 1998.

- Cement and Concrete Reference Laboratory (CCRL).

E. Concrete Reinforcing Steel Institute (CRSI).

1.  CRSI - Manual of Standard Practice; 2001.

F. Department of Defense (DOD).

- DOD P-21035A - Galvanizing Repair Specification.

G. Precast/Prestressed Concrete Institute.

1. PCI MNL-117 - Manual for Quality Control for Plants and Production of Architectural

Precast Concrete Products; 1996.

H. Steel Structures Painting Council (SSPC).

1. SSPC Paint 20 - Zinc-Rich Primers (Type I, Inorganic, and Type II, Organic); 2002.

2. SSPC Paint 25 - Zinc Oxide, Alkyd, Linseed Oil Primer for Use Over Hand Cleaned

Steel, Type I and Type II; 1997.

I. American Institute of Steel Construction (AISC).

1.4 SUBMITTALS

A. Submit under provisions of Section 01300.

B. Product Data: Submit product data for manufactured materials and products.

C. Shop Drawing:

1. Show in-place location, manufacturing details, plans, elevations, anchorages,

reinforcement, connection details and methods, dimensions, finishes, relationships to

adjacent materials, and erection and placement.

2. Show identification marks, coordinated to Shop Drawings, and date of manufacture on

all units to facilitate hauling and erection.

3. Setting diagrams, templates, instructions and directions as required for installation.

D. Engineering Calculations: Engineering calculations as required sealed by an engineer

licensed to practice in (project state).

E. Mix Design(s): Proposed concrete mix design for each type and color of concrete mix

required including backup mix.

F. Material Test Reports: Submit material certificates signed by manufacturer for concrete

materials, reinforcing materials, admixtures, and similar items.

G. Certifications:

1. Manufacturer’s certification from APA, PCI, or applicable municipal certifications.

2. Welder’s AWS certification. Submit for each welder.

H. Selection Samples: For each finish product specified, two complete sets of color chips

representing manufacturer's full range of available colors, textures, and patterns.

I. Verification Samples: For each finish product specified, two samples, approximately 12

inches (300 mm) square, representing actual product, color, texture, and patterns.

1.5 QUALITY ASSURANCE

A. Manufacturer’s Qualifications.

1.  Firm shall have a minimum of five years experience in producing units similar to those

required for this Project, with sufficient production capacity to produce and deliver

required units without causing delay in Work.

2. Fabricating plant shall be certified by one of the following:

a. Architectural Precast Association (APA).

b. Precast/Prestressed Concrete Institute (PCI), Group A1.

c. Or Equal Certification Program.

B. Installer’s Qualifications: Installer shall have a record of at least five years of successful

installation of units similar to those required for this Project.

C. Welder’s Qualifications: Provide certification that welders to be employed in the Work are

certified by AWS and applicable local building officials, and have been re-certified in the last

12 months.

D. Mock-Up: Provide a mock-up for evaluation of surface finishes and workmanship.

1. Provide initial production units for job-site assembly with other materials for approval.

Coordinate type and location of mock-ups with project requirements. Accepted units

will be used as the standard for acceptance of production units. Remove and replace

units which are not accepted.

2. Do not proceed with remaining work until workmanship, color, and finish are approved

by Architect.

3. Refinish mock-up area as required to produce acceptable work.

- Incorporate accepted mockup as part of Work.

1.6 DELIVERY, STORAGE, AND HANDLING

A. Deliver, store and handle precast in strict compliance with manufacturer's instructions and

recommendations and industry standards Protect from damage. Lift and support units only

at designated lifting points as shown on approved Shop Drawings.

B. Deliver units to the Project site in such quantities and at such times to ensure continuity of

installation.

C. Handle precast units to position, consistent with their shape and design. Lift and support

only from support points.

D. Provide anchorage items to be embedded in or attached to other construction without

delaying the Work. Provide setting diagrams, templates, instructions and directions as

required for installation.

E. Blocking and Lateral Support During Transport and Storage: Clean, non-staining, without

causing harm to exposed surfaces. Provide temporary lateral support to prevent bowing

and warping.

F. Protect units to prevent staining, chipping, or spalling of concrete.

G. Mark units with date of production in location not visible to view when in final position in

structure.

PART 2 PRODUCTS

2.1 MANUFACTURERS

A. Acceptable Manufacturer: Advanced Cast Stone Inc., 115 Lee Street, Everman, TX. 76140 Tel: (800) 687-4352, Fax: (817) 293-6378. Email: DebbieC@advancedcaststone.com  Website: www.advancedcaststone.com

B. Substitutions: Not permitted.

C. Requests for substitutions will be considered in accordance with provisions of Section

01600.

2.2 APPLICATIONS/SCOPE

A. Design units to withstand design loads as calculated in accordance with applicable code,

and erection forces. Calculate structural properties of units in accordance with ACI 318.

1. Wind Loads.

2. Seismic forces.

3. Building dynamics, thermal, live, impact or concentrated loads, structural deflection,

story drift.

2.3 MATERIALS

A. Concrete Materials:

1. Portland Cement: Complying with ASTM C 150, Type I or III, white or gray colors to

achieve desired finish colors. Use only one brand, type, and color from the same mill.

Gray cement may be used for non-exposed backup mixes.

2. Aggregates: Complying with ASTM C 33, gradation may differ to achieve desired

finish characteristics. Select coarse and fine aggregate colors and screen sizes to

match approved sample(s). Verify that adequate supply, from one pit or quarry, for

each type of aggregate is available for the entire Project. If possible obtain entire

aggregate supply prior to starting Work, or have aggregate supply held in reserve by

aggregate supplier.

3. Lightweight aggregate: Complying with ASTM C 330.

4. Water: Potable. Clean, clear, and free from deleterious amounts of salts, acids,

alkalies, organic materials, oils, detergents, or other matter that may interfere with

color, curing, or strength of concrete.

5. Admixtures: Select to be compatible in specified mix.

a. Air Entraining: Complying with ASTM C 260.

b. Water Reducing: Complying with ASTM C 494, Type A, B, C, For G.

c. Silica Fume: Complying with ASTM C 1240, for cement replacement for high

performance concrete.

d. Coloring Agent: Complying with ASTM C 979, compatible with other concrete

materials.

e. Other constituents: Integral water repellents and other chemicals for which no

ASTM standard exists, shall be previously established as suitable for use in

concrete or shall be shown by test or experience not to be detrimental to the

concrete.

B. Formwork:

1. Provide forms with acceptable form facing materials that are non-reactive with

concrete or form release agents and will produce required finish surfaces.

2. Construct and maintain forms to produce precast concrete units of shapes, lines, and

dimensions indicated, within specified tolerances.

C. Reinforcing Materials:

1. Reinforcing Bars: Complying with ASTM A 615/A 615M, Grade 40 or 60, unless

otherwise required to meet structural requirements.

2. Galvanized Reinforcing Bars: Complying with ASTM A 767/A 767M, hot-dip

galvanized; use where concrete cover is less than 1-1/2 inches.

3. Epoxy Coated Reinforcing Bars: Complying with ASTM A 934; use in special

applications where indicated.

4. Steel Welded Wire Fabric: Complying with ASTM A 185, plain, cold drawn.

5. Pre-Stressing Tendons: Complying with ASTM A 416/A 416M, Grade 250 or 270, uncoated,

7 wire, low relaxation strand.

D. Connection Materials:

1. Steel Shapes and Plates: Complying with ASTM A 36/A 36M.

2. Malleable Iron Castings: Complying with ASTM A 47/A.47M.

3. Carbon Steel Plates: Complying with ASTM A 283/A 283M.

4. High Strength, Low Alloy Structural Steel: Complying with ASTM A 572.

5. Carbon Steel Structural Tubing: Complying with ASTM A 500, Grade B.

6. Anchor Bolts: Complying with ASTM A 307, carbon steel or ASTM A 325 (ASTM

A325M), high strength; bolts nuts, and washers.

7. Welded Headed Studs: Complying with AWS D1.1/D1.3M, Type B.

8. Deformed Steel Wire Bar Anchors: Complying with ASTM A 496.

9. Stainless Steel Plate: Complying with ASTM F 593, Type 304 or Type 316; bolts and

studs, nuts and washers. Note that selection of stainless steel will result in increased

costs.

10. Finish for Steel Connection Materials:

a. Hot-dip galvanize steel exposed to weather in final assembly complying with

ASTM A 123/A 123M or ASTM A 153/A 153M.

b. Shop Prime Remaining Steel Shapes: Complying with SSPC Paint 25.

c. Anchor Bolts, Nuts, Washers, Cadmium Plated: Complying with ASTM A 563,

Grade C.

d. Hot-dip galvanize setting bolts or projecting steel in masonry applications

complying with ASTM A 153/A 153M.

e. Galvanizing Repair Paint: Complying with DOD P-21035A or SSPC Paint 20.

f. Welding Electrodes: Comply with AWS Standards.

E. Bearing Pads: Elastomeric pads, complying with ASTM D 412.

F. Grout Materials:

1. Cement Grout: Cement complying with ASTM C 150; sand complying with ASTM C

404; proportions 1:2.5 by volume, minimum water for placement and hydration.

2. Non-Shrink Grout: Complying with ASTM C 1107.

3. Epoxy Grout: Consult Suppliers.

2.4 MIXES

A. Design mixes for each type of concrete specified shall be prepared by an independent

testing agency or by an architectural precast manufacturing plant at precast manufacturer’s

option. Proportion mixes by either testing agency trial batch or field test data methods in

accordance with ACI 211.1, using materials to be used on the Project, to provide concrete

with properties as follows:

1. Concrete Density: Normal weight.

2. Concrete Density: Lightweight.

3. Compressive Strength: 5,000 psi (35 MPa) when tested in accordance with ASTM C

39/C 39M.

4. Maximum water cement ratio 0.40 at point of placement.

5. Add air-entrainment admixture to result in air content at point of placement complying

with ACI 533R requirements.

6. Water absorption maximum 6% (by weight) when tested in accordance with ASTM C

642.

2.5 MANUFACTURING

A. General:

1. Fabricate precast concrete units with manufacturing and testing procedures, quality

control recommendations, and dimensional tolerances as specified in PCI MNL-117

or ACI 533R, unless more stringent requirements are shown or specified.

2. Fabricate units straight, smooth and true to size and shape, with exposed edges and

corners precise and square, unless otherwise indicated.

B. Cast openings larger than 10 inches (254 mm) in any dimension according to locations

shown on Shop Drawings. Smaller holes may be field cut when approved by Architect.

C. Reinforcement: Comply with CRSI Manual of Standard Practice, PCI MNL-117, or ACI 533R

recommendations. Reinforce architectural precast concrete units to resist handling,

transportation, and erection stresses, and to comply with specified performance criteria.

D. Pretension tendons for units in compliance with PCI MNL-117 or ACI 533R.

E. Cast-in Items: Provide embedded anchors, inserts, steel shapes, and lifting devices as

shown on reviewed Shop Drawings. Window connections are best made by field drilled

inserts. Firmly hold cast items in place by jigs, strongbacks, or other approved means.

F. Comply with PCI MNL-117 or ACI 533R requirements for measuring, mixing, transporting,

and placing concrete. Place facing mix to a thickness of the greater of 1 inch (26 mm) or 1.5

times the maximum aggregate size. Place back-up concrete to ensure bond with face

concrete.

G. Consolidate concrete using equipment and procedures complying with PCI MNL-117 or ACI

533R.

H. Permanently mark units with pick-up points as shown on reviewed Shop Drawings. Imprint

casting date and piece mark on a surface to be concealed from view in the finished

structure.

I. Cure concrete in accordance with PCI MNL-117 or ACI 533R requirements.

J. Discard units that are warped, cracked, broken, spalled, stained, or otherwise defective

unless repairs are approved by the Architect and meet specified requirements. Refer to ACI-

533R for product finish requirements unless otherwise shown or specified.

K. Manufacturing Tolerances: Fabricate to tolerances listed in PCI MNL-117 or ACI 533R.

2.6 FINISHES

A. Finish exposed surfaces or units to match Architect’s design reference sample.

B. Finish exposed surfaces or units to match APA and PCI “Architectural Precast Concrete-

Color and Texture Selection Guide” of Plate Numbers Indicated.

C. Finish exposed surfaces or units in accordance with the following:

1. Smooth surface finish free from pockets, sand streaks, honeycomb, with uniform color

and texture. State whether bugholes less than 5/8 inch (16 mm) in diameter are

acceptable.

2. Textured surface finish from form liners or inserts.

3. Machine textured finish, using power or hand tools to remove matrix and fracture

coarse aggregate.

4. Retarded finish, using chemical retarding agents applied to forms, with washing and

brushing procedures to expose aggregate and surrounding matrix.

5. Abrasive blast finish, using abrasive grit, equipment, application and cleaning

procedures to expose aggregate and surrounding matrix.

6. Acid etched finish using acid solution and application techniques to expose aggregate

and surrounding matrix.

7. Honed or Polished finish using mechanical abrasion, followed by filling and rubbing

procedures.

8. Sand embedment finish, using selected coarse aggregate placed in a sand bed in the

bottom of the mold, with sand removed after removal from the mold.

9. Applied material finish, using selected ceramic or natural stone materials, specified in

Section 04400.

D. Finish Exposed Back Surface of Units:

1. To match face surface of units.

2. By smooth, steel trowel finish.

E. Finish unexposed surfaces of units by float finish or as-cast form finish.

2.7 SOURCE QUALITY CONTROL

A. Inspect and test architectural precast concrete in accordance with PCI MNL-117 or ACI

533R.

B. The Owner may retain an independent Testing Laboratory to evaluate manufacturer’s quality

control and testing methods. Testing Laboratory shall be certified by CCRL or similar

National authority. Manufacturer shall allow Testing Laboratory access to all operations

pertinent to the Project.

C. Defective Work: Discard units that do not conform to requirements as shown or specified.

Replace with units which meet requirements.

PART 3 EXECUTION

3.1 EXAMINATION

A. Do not begin installation until substrates have been properly prepared.

B. Field Dimensions: Furnish field dimensions to manufacturer as required.

C. Examine substrates and conditions for compliance with requirements for installation,

tolerances, true and level bearing surfaces, and other conditions affecting performance of

architectural precast concrete units.

D. If substrate preparation is the responsibility of another installer, notify Architect of

unsatisfactory preparation before proceeding.

E. Do not install units until supporting structure has been completed and has attained minimum

allowable design compressive strength.

3.2 ERECTION

A. Erect units using personnel experienced and trained in placement and securing of precast

concrete units.

B. Lift and handle precast using lift points and embeds as shown on approved shop drawings.

C. Erect level, plumb, and true to line. Do not allow cumulative dimensional errors to develop.

1. Adjustments such as shimming which would place additional stress on units shall not

be permitted.

2. Adhere to dimensional tolerances in accordance with PCI recommendations.

D. Erect and secure in a manner to prevent damage to units or units in place.

E. Erection Tolerances. Erect within tolerances listed in PCI MNL-117 Appendix I or ACI 533R.

F. Joint Sealants: As specified in Section 07900.

G. Where two stage joint seal is required, sequence with sealant application to ensure that

sealant, gaskets, and similar items required for interior side seal are installed concurrently

with installation of precast units.

3.3 CLEANING

A. Clean exposed surfaces of units after erection if soiled or stained.

1. Wash and rinse according to architectural precast concrete manufacturer’s

recommendations. Protect other work from damage while cleaning.

2. Do not use cleaning materials or methods that change the appearance of architectural

precast concrete finishes. Test clean a small area to verify adequacy and safety of

materials and methods.

3. Leave in condition for application of water repellents specified in Section 07190.

3.4 PROTECTION

A. Subsequent trades to Protect finished surfaces from soiling or damage.

B. Touch-up, repair or replace damaged products before Substantial Completion.

1. Repair exposed surfaces of units to match color, texture, and uniformity of

surrounding units.

2. Remove and replace damaged units when repairs do not meet requirements.

3.5 SCHEDULE

A. Item: