Advanced Cast Stone’s GFRC

Standard Specifications

SECTION 03490

GLASS-FIBER REINFORCED PRECAST CONCRETE

PART 1 GENERAL

1.1 SECTION INCLUDES

A. Plant-cast, glass-fiber-reinforced precast concrete panels.

B. Embedded hardware and anchors.

C. Loose connection hardware.

D. Integrated steel support framing.

1.2 RELATED SECTIONS

A. Section 03300 - Cast-in-Place Concrete: Building structural frame.

B. Section 04800 – Unit Masonry: Back-up masonry.

C. Section 05120 - Structural Steel: Building structural frame.

D. Section 05400 - Cold-Formed Metal Framing: Structural stud members.

E. Section 07190 - Water Repellent Coating.

F. Section 07600 - Metal flashings.

G. Section 07840 - Firestopping: Fire barrier seal between units and edge of floor slab.

H. Section 07900 - Joint Sealers: Application of backer rods or bond breakers and joint

sealers.

1.3 REFERENCES

A. ASTM A 27/A 27M – Standard Specification for Steel Castings, Carbon for General

Application.

B. ASTM A 36/A 36M – Standard Specification for Carbon Structural Steel.

C. ASTM A 47/A 47M – Standard Specification for Ferritic Malleable Iron Castings.

D. ASTM A 123/A 123M - Standard Specification for Zinc (Hot-Dip) on Iron and Steel

Hardware.

E. ASTM A 108 – Standard Specification for Steel Bars, Carbon, Cold-Finished, Standard

Quality.

F. ASTM A 153/A 153M - Standard Specification for Zinc Coating (Hot-Dip Galvanized)

Coatings on Iron and Steel Products.

G. ASTM A 283/A 283M - Standard Specification for Low and Intermediate Tensile Strength

Carbon Steel Plates.

H. ASTM A 325 - Standard Specification for Structural Bolts, Steel, Heat Treated, 120/105 ksi

Minimum Tensile Strength.

I.  ASTM A 500 - Standard Specification for Cold-Formed Welded and Seamless Carbon    Steel Structural Tubing in Rounds and Shapes.

J. ASTM A 513 - Standard Specification for Electric-Resistance-Welded Carbon and Alloy

Steel Mechanical Tubing

K. ASTM A 653/A 653M - Standard Specification for Steel Sheet, Zinc-Coated (Galvanized)or

Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process.

L. ASTM A780 - Standard Practice for Repair of Damaged and Uncoated Areas of Hot-Dip

Galvanized Coatings.

M. ASTM A1003/A1003M - Standard Specification for Steel Sheet, Carbon, Metallic- and

Nonmetallic-Coated for Cold-Formed Framing Members.

N. ASTM A1008/A1008M - Standard Specification for Steel, Sheet, Cold-Rolled, Carbon,

Structural, High-Strength Low-Alloy and High-Strength Low-Alloy with Improved   Formability.

O. ASTM C 33 - Standard Specification for Concrete Aggregates.

P. ASTM C 150 - Standard Specification for Portland Cement.

Q. ASTM C 260 - Standard Specification for Air-Entraining Admixtures for Concrete.

R. ASTM C 494/C 494M - Standard Specification for Chemical Admixtures for Concrete.

S. ASTM C 618 - Standard Specification for Coal Fly Ash and Raw or Calcined Natural

Pozzolan for Use as a Mineral Admixture in Portland Cement Concrete.

T. ASTM C 979 - Standard Specification for Pigments for Integrally Colored Concrete.

U. ANSI - American Iron and Steel Institute (AISI), Specification for the Design of Cold- Formed Steel Structural Members

V. AWS D1.1 - Structural Welding Code - Steel.

W. AWS D1.3 - Structural Welding Code - Sheet Steel.

X. AWS D1.4 - Structural Welding Code - Reinforcing Steel.

Y. PCI MNL-117 – Manual for Quality Control for Plants and Production of Architectural Precast Concrete Products.

Z. PCI MNL-128 – Recommended Practice for Glass Fiber Reinforced Concrete Panels.

AA. PCI MNL-130 – Manual for Quality Control for Plants and Production of Glass Fiber

Reinforced Concrete Products.

BB. SSPC 2 – Hand Tool Cleaning.

CC. SSPC 3 – Power Tool Cleaning.

DD. SSPC Paint 20 - Zinc-Rich Primers (Type I - Inorganic and Type II - Organic).

EE. SSPC Paint 25 - Zinc Oxide, Alkyd, Linseed Oil Primer for Use Over Hand Cleaned   Steel, Type I and Type II

FF. CIELAB - International Commission of Illumination, 1976 Standards.

1.4 SYSTEM DESCRIPTION

A. System: Plant fabricated glass-fiber-reinforced precast concrete panels consisting of face

mix, back-up mix, steel support frame attached via pins, gravity anchors and flex anchors,

steel connections for panel attachment to structure, and other inclusions for attachments to

panels.

B. Design Requirements: Design glass-fiber-reinforced precast concrete panels and shapes

under the supervision of a professional engineer and in accordance with procedures of PCI

MNL-128, Recommended Practices for Glass Fiber Reinforced Concrete Panels using

property data generated from the manufacturer’s actual production.

C. Performance Requirements:

1. Provide glass-fiber-reinforced precast concrete panels and panel frames capable of

withstanding gravity, wind, seismic, and erection design loads as well as the effects of

thermal and moisture-induced volume changes, according to load factors and

combinations established in PCI MNL 128.

2. Design Loads: As indicated.

3. Design framing systems to withstand design loads with lateral deflections no greater

than 1/240 of the wall height.

4. Provide for movement of framing members without damage or overstressing,

connection failure, undue strain on fasteners and anchors, or other detrimental effects

when subject to a maximum ambient temperature change of 100 degrees F.

1.5 SUBMITTALS

A. Submit under provisions of Section 01300.

B. Product Data: Submit manufacturer's data sheets on each product to be used, including:

1. Preparation instructions and recommendations.

2. Storage and handling requirements and recommendations.

3. Installation methods.

C. Shop Drawings: Indicate dimensions, cross-sections and edge details; metal framing  details, location, size and type of reinforcement, including reinforcement necessary for safe handling and erection; and connection details, and relationship to adjacent materials:

1. Design calculations demonstrating compliance with indicated loading conditions and

showing flexural ultimate strengths assumed for design, stamped by a structural

professional engineer registered in the location of the project.

2. Layout, dimensions, and identification of each panel segment corresponding to

installation sequence.

3. Location and details of anchorage devices embedded in panels and shapes, and

connection details to building.

D. Samples:

1. Selection Samples: For each finish product specified, two complete sets of color

sample, minimum size 6 inches (150 mm) square, representing manufacturer's full

range of available colors and patterns for the exposed face of panels.

2. Verification Samples: For each finish product specified, two samples, minimum size 6

inches (150 mm) square, representing actual product, color, and patterns for the

exposed face of panels.

3. Do not start fabrication until samples are approved.

E. Maintain plant records and quality control program during production of units. Make     records and access to plant available to Architect upon request.

F. Submit certificates of compliance for the following:

1. Admixtures.

2. Portland Cement: Identify the cement brand name, type and mill location used for the

quality control sample.

3. Glass Fibers: Submit evidence that glass composition, Portland cement matrix, or

both have been designed for glass-fiber reinforced precast concrete panel

applications.

1.6 QUALITY ASSURANCE

A. Perform Work in accordance with PCI MNL 128, Recommended Practice for Glass Fiber

Reinforced Concrete Panels

B. Manufacturer Qualifications: Provide panels and shapes only from a manufacturer who   has demonstrated capability to produce products of the quality and scope required for this project, and with not less than 5 years of successful experience in manufacturing glass-fiber reinforced precast concrete panels and shapes and who is certified in one or more of the following programs:

1. Certified Participant in the Architectural Precast Association’s Plant Certification

Program for GFRC.

2. Designated PCI-Certified Plant for Group G, Glass Fiber Reinforced Concrete by

PCI’s Plant Certification Program

3. Retains licensed Professional Engineer for plant and record inspection indicating

production, testing and quality control methods comply with PCI MNL-130, Manual for

Quality Control: Glass Fiber Reinforced Concrete.

C. Installer Qualifications: A firm which has specialized in erection of glass-fiber reinforced

precast concrete panels or architectural precast concrete items similar to those required on

this project for not less than 5 years and who is acceptable to manufacturer of glass-fiber

reinforced precast concrete panels.

D. Welder Qualifications: Use welders who have been qualified in accordance with AWS D1.1

and AWS D1.4 within the last year.

E. Mock-Up: Provide a mock-up for evaluation of surface preparation techniques and

application workmanship.

1. Finish areas designated by Architect.

2. Do not proceed with remaining work until workmanship, color, and sheen are

approved by Architect.

3. Refinish mock-up area as required to produce acceptable work.

1.7 DELIVERY, STORAGE, AND HANDLING

A. Deliver units to the project site palletized, safely wrapped, packed and labeled and retain

until erected.

B. Store materials in a dry location off the ground, and in such a manner to prevent damage    or intrusion of foreign matter.

C. Handle and transport units in a position consistent with their shape and design in order to

avoid excessive stresses or damage.

D. Store units to protect them from contact with soil, staining, and from physical damage.

E. Place stored units so that identification marks are easily readable.

PART 2 PRODUCTS

2.1 MANUFACTURERS

- Acceptable Manufacturer: Advanced Cast Stone Inc. 115 Lee Street, Everman, TX. 76140  Tel: (800) 687-4352 Fax: (817) 293-6378. Email: DebbieC@advancedcaststone.com Website: www.advancedcaststone.com

B. Substitutions: Not permitted.

C. Requests for substitutions will be considered in accordance with provisions of Section

01600.

2.2 MATERIALS

A. Aggregates:

1. Back-up Mix: Washed and dried silica sand or other sand having a history of

successful use in glass-fiber-reinforced precast concrete panel construction; passing

through a No. 20 sieve.

2. Facing Mix: Fine and course aggregate for face mix shall conform to ASTM C 33

except for gradation. Aggregates shall be clean, hard, strong, durable, inert, and free

of staining and deleterious materials. Provide aggregate in colors and sizes as

required to achieve the panel finish texture and colors indicated on the Drawings.

B. Portland Cement: ASTM C 150, Type I, II or III. Use the same type, brand and color of

portland cement for all panels and shapes. Color shall be as required to obtain the panel

facing color indicated.

C. Admixtures:

1. Air-entraining admixtures, ASTM C 260. ASTM C260, ASTM C494, ASTM C618 or

acrylic thermoplastic copolymer dispersion conforming to PCI MNL-130, Appendix E.

2. Polymer Compound: Conform to requirements of PCI MNL-128, Appendix L.

D. Coloring Agent: ASTM C 979; shall have no adverse effects to glass-fiber-reinforced     precast concrete panel set and strength; shall be stable at high temperature; and shall be sunlight fast and alkali-resistant. Color shall be as required to obtain panel facing color selected.

E. Water for Mixing Concrete: Use potable water.

F. Glass Fiber: Conforming to PCI MNL-130, Appendix D and specifically designed to be

compatible with the aggressive alkaline environment of portland cement based composites

or fibers with a history of successful use in portland cement based composites that has      been modified to be compatible with the fiber.

G.  Anchors and Loose Attachment Hardware:

1. Structural Steel: ASTM A 36/A 36M.

2. Cold Drawn Wire:

3. Anchor Bolts: ASTM A 325.

4. Pipe: ASTM A 500 Grades A or B.

5. Tube Steel: ASTM A 500 Grade A or B.

6. Carbon-Steel Rods: ASTM A 108, cold drawn.

7. Carbon-Steel Plate: ASTM A 283/A 283M.

8. Malleable-Steel Castings: ASTM A 47/A 47M.

9. Carbon-Steel Castings: ASTM A 27/A27M, Grade 60-30.

10. Finish: Galvanized in accordance with ASTM A 153/A 153M.

H. Panel Frame Materials:

1. Cold-Formed Steel Framing: Manufacturer's standard C-shaped steel studs,

complying with AISI "Specification for the Design of Cold-Formed Steel Structural

Members," minimum uncoated steel thickness of 0.0538 inch (1.37mm) of web depth

indicated, with stiffened flanges, V-shaped steel track, and of the following steel

sheet:

a. Metallic-Coated Steel Sheet: ASTM A 653/A653M, structural-steel sheet, of

grade required by structural performance of framing and with zinc coating

thickness of:

1) G60 (Z180).

2) G90 (Z275).

b. Painted, Nonmetallic-Coated Steel Sheet: ASTM AlOll/AlOllM hot rolled or

ASTM AlO08/ AlO08M cold rolled; nonmetallic coated according to ASTM A

1003/ A 1003M; of grade required by structural performance of framing.

2. Hollow Structural Sections: Steel tubing, ASTM A500, Grade B, or ASTM A5l3. Finish

hollow structural sections with wall thickness less than 3/16 inch (4.76 mm) as

follows:

a. Organic Zinc-Rich Primer: SSPC-Paint 20 on surfaces prepared to comply with

SSPC-SP6/NACE No.3, "Commercial Blast Cleaning."

b. Primer: SSPC-Paint 25 on surfaces prepared to comply with SSCP-SP 2, Hand

Tool Cleaning," or better.

3. Steel Channels and Angles: ASTM A36/ A36M, finished as follows:

a. Organic Zinc-Rich Primer: SSPC-Paint 20 on surfaces prepared to comply with

SSPC-SP6/NACE No.3, "Commercial Blast Cleaning."

b. Primer: SSPC-Paint 25 on surfaces prepared to comply with SSCP-SP 2,

"Hand Tool Cleaning," or better.

I.  Form Materials: Provide form materials that will produce panels having the profile,

dimensions and tolerances indicated. Use release agents which are compatible with finish

specified and joint sealants proposed for use.

J. Mixes: Portland cement, water, glass fibers and sand mixed in proportions determined in

accordance with PCI MNL-128.

2.3 FABRICATION

A. Fabricate panels in general compliance with PCI MNL-128 and MNL-130.

B. Molds:

1. Rigid and constructed of materials that will result in finished products conforming to

the profiles, dimensions and tolerances indicated on the Drawings.

2. Release agents; apply and use according to manufacturer’s instructions.

C. Proportioning and Mixing:

1. Carefully measure mix constituents in a manner to achieve the desired mix

proportions.

2. Meter the glass fiber and cement slurry to the spray head at rates to achieve the

desired mix proportion and glass content. Check rates in accordance with standard

procedures described in PCI MNL-128.

3. Maintain cleanliness of equipment and working procedures at all times.

D. Hand Spray Application:

1. Spray apply a mist coat consisting of the matrix without fiber. Applied coating not to

exceed 1/8 inch thick in order to avoid an un reinforced surface.

2. Spray or place face mix in thickness shown on shop drawings.

3. Spray-up main body of material before the mist coat has set.

4. Apply by spraying such that uniform thickness and distribution of glass fiber and

cement matrix is achieved during the application process.

5. Consolidate by rolling or such other techniques as necessary to achieve complete

encapsulation of fibers and compaction.

6. Control thickness by using a pin gauge or other approved method. Perform a

minimum of 2 measurements per 5 square feet of panel surface with at least 3

measurements per panel.

7. Perform hand forming of intricate details, incorporate formers or infill material, and

overspray before the material has achieved its initial set so as to insure complete

bonding.

E. Inserts and Embedments:

1. Properly embed inserts in built up homogeneous glass-fiber reinforced precast

concrete panel bosses to develop their strength. Waste material or overspray is not

acceptable to encapsulate inserts or for bonding pads.

2. Test inserts to establish test data and reduce test values by the appropriate safety

factors to determine connection strength to be used in design.

3. Rigid embedded items bonded to the glass-fiber reinforced precast concrete panel

shall not create undesirable restraint to volume changes.

F. Panel Frame Fabrication:

1. Fabricate panel frames and accessories plumb, square, true to line, and with

components securely fastened in accordance with design requirements.

a. Fabricate panel frames using jigs or templates.

b. Cut cold-formed metal framing members by sawing or shearing; do not torch

cut.

c. Fasten cold-formed metal framing members by welding. Comply with AWS

D1.3 requirements and procedure for welding, appearance and quality of

welds, and methods used in correcting welding work.

d. Fasten framing members of hollow structural sections, steel channels, or steel

angles by welding. Comply with AWS DI.I requirements and procedures for

welding, appearance and quality of welds, and methods used in correcting

welding work.

e. Weld flex, gravity, and seismic anchors to panel frames.

2. Reinforce, stiffen, and brace framing assemblies, if necessary, to withstand handling,

delivery, and erection stresses. Lift fabricated assemblies in a manner that prevents

damage or significant distortion.

3. Galvanizing Repair: Touch up accessible damaged galvanized surfaces according to

ASTM A 780.

G. Finish of Exposed Faces: Panel faces shall be free of honeycombs, form marks, concrete

droppings or other blemishes that would telegraph through the panel. Provide a finish

surface free of laitance, grease, form release treatments, efflorescence, curing compounds

or other foreign material that would adversely affect bonding of any subsequent coating.

1. Color and texture of exposed face surfaces shall match Architect’s design reference

panel.

2. Color and texture of exposed face surfaces shall match _____________.

3. Color and texture of exposed face surfaces shall match one of the manufacturers

standard finishes as selected by the Architect.

H. Dimensional Tolerances of Finished Units: Provide in accordance with PCI MNL-117 and

PCI MNL-128.

I.  Cover: Provide embedded anchors, inserts, and other sprayed in items with sufficient

anchorage and embedment for design requirements.

J. Curing:

1. Immediately after the completion of spraying of the panel, cure panels using a method

to ensure sufficient strength for removing the units from the form.

2. After initial curing, remove panel from form and place in a controlled curing

environment.

3. An acrylic thermoplastic copolymer dispersion may be used as a curing admixture.

Only copolymers shown to eliminate the need for moist curing through independent

laboratory test data shall be used.

K. Panel Identification:

1. Mark each glass-fiber reinforced precast concrete panel to correspond to identification

mark on shop drawings for panel location.

2. Mark each glass-fiber reinforced precast concrete panel with date on which it was

cast.

3. Apply markings on surface that will not be exposed in the finished construction.

2.4  SOURCE QUALITY CONTROL

A.  Independent Testing:

1. Allow Owner's testing agency access to material storage areas, concrete production

equipment, concrete placement, and curing facilities.

2. Cooperate with Owner's testing agency and provide samples of materials and

concrete mixes as may be requested for additional testing and evaluation.

3. Test glass-fiber reinforced precast concrete panel units in accordance with PCI MNL-

130.

B. Plant Testing:

1. Test glass-fiber reinforced precast concrete panel units in accordance with PCI MNL-

130.

2. Perform testing by an independent testing agency capable of performing the specified

tests. Submit copies to the Architect and designated authorities.

C. Acceptability of Appearance:

1. Finished construction in place shall present a uniform, pleasing appearance when

viewed in good typical lighting with the naked eye at a distance of 10 feet and shall

show no imperfections at a distance of 20 feet.

2. The range of total acceptable color (lightness, color saturation and hue) variation shall

not exceed CIELAB 3.0 provided that the difference in hue alone does not exceed

CIELAB 1.0 as defined by the International Commission of Illumination, 1976

Standards.

PART 3 EXECUTION

3.1 EXAMINATION

A. Check placement of structural support system to assure a true and level surface for

attachment of panels. Do not begin construction until discrepancies that could adversely

affect installation of panels have been corrected.

B. If substrate preparation is the responsibility of another installer, notify Architect of

unsatisfactory preparation before proceeding.

3.2 PREPARATION

A. Clean surfaces thoroughly prior to installation.

B. Prepare surfaces using the methods recommended by the manufacturer for achieving the

best result for the substrate under the project conditions.

3.3 INSTALLATION

A. Install in accordance with manufacturer's instructions.

B. Setting:

1. Lift glass-fiber reinforced precast concrete panel units with suitable lifting devices at

points provided by the manufacturer.

2. Set glass-fiber reinforced precast concrete panel units level, plumb, square and true

within the allowable tolerances.

3. Site cutting of panels is not permitted.

C. Supports and Bracing: Provide temporary supports and bracing required to maintain

position, stability, and alignment as units are being permanently connected.

D. Fastening:

1. Fasten glass-fiber reinforced precast concrete panel units in place by bolting or

welding or both as shown on erection drawings.

2. Field welding shall be done by qualified welders using equipment and materials

compatible with the base material.

3. Use non-combustible shields during welding operations to protect adjacent Work.

E. Tolerances of Erected Units:

1. Tolerances for location of glass-fiber reinforced precast concrete panel units shall be

noncumulative and as listed below. For erection tolerances not listed below, those

listed in PCI MNL 117 shall apply.

2. Face width of joint:

a. Panel dimension 10 feet or less plus 3/16 inch.

b. Panel dimension 10 to 20 feet plus 3/16 inch, minus 1/4 inch.

c. Panel dimension greater than 20 feet plus 1/4 inch, minus 5/16 inch

3. Warpage: Maximum permissible warpage of one corner out of plane of the other three

shall be 1/16 inch per foot of distance from the nearest adjacent corner or 1/8 inch

total after installation.

4. Bowing: Not over L/360, where L is the panel length.

3.4 PATCHING AND CLEANING

A. Patch and clean panels using methods and materials in accordance with manufacturer's

instructions.

B.  Patching blemishes using a patching mixture matching the color and texture of   surrounding surface.

C.  Use extreme care to prevent damage to panel surfaces and to adjacent materials. Provide

protection of adjacent surfaces if required.

D.  Surface must be thoroughly rinsed with clean water immediately after using cleaner.

3.5 FIELD TESTS AND INSPECTION

A.  Quality Control Program: Panel manufacturer shall have an established quality control

program if effect at the plant or shall employ an independent testing laboratory approved     by the Architect to monitor glass content, spray rate, physical properties and curing period and conditions.

B. Sampling and Testing:

1. Prepare test specimens and use test procedures in accordance with PCI MNL-128,

Chapter 8 and Appendix A.

2. Prepare a minimum of 2 test boards per work shift until a production uniformity

acceptable to the quality control personnel has been achieved. At such time

frequency may be reduced to one board per work shift.

3. For each board determine glass content by the washout test, flexural ultimate strength

and flexural yield strength.

4. Glass content shall be considered satisfactory if within minus 0.5 and plus1.0 percent,

by weight, of the glass content in the design mix.

5. Flexural yield strength shall be considered satisfactory if both of the following

requirements are met.

a. The average of all sets of 3 consecutive strength tests equal or exceed

assumed ultimate flexural strength for design purposes.

b. No individual test (average of 6 coupons) fall below required assumed ultimate

flexural strength for design purposes by more than 10 percent.

6. Submit reports giving proportions, test results, inspection results, unit identification

numbers and casting date for each work shift.

C. Rejection:

1. Panels in place may be rejected for any one of the following product defects or

installation deficiencies:

a. Non-repairable damage incurred during construction operations.

b. Ragged or irregular edges.

c. Visible form joints or irregular surfaces.

d. Panels not conforming to tolerance requirements.

e. Foreign material embedded in the face.

f. Visible repairs.

g. Cracks visible at a distance of 10 feet.

h. Panels do not meet design strength requirements.

3.6 PROTECTION

A. Protect installed products until completion of project.

B. Touch-up, repair or replace damaged products before Substantial Completion.

3.7 SCHEDULE

A. Item: